广州同怡新材料科技有限公司


YWU2569S

Product introduction

   YWU2569S is di-functional polyurethane acrylic oligomer, the molecular weight between 2700-5400, low molecular functionality, excellent adhesion and flexibility, show the material macro excellent performance, such as excellent adhesion and toughness, high gloss and yellowing resistance, weather resistance and excellent chemical resistance, because the main functional groups containing allyl base double bond, can radiation curing or chemical crosslinking, products with shallow transparent color, high adhesion scratch resistant, no yellowing highlights; The wide range of applications, can separate as main resin used for UV glue, uv-curable coatings and printing ink and other products, and can and other acrylic system, epoxy, polyurethane, nitrocellulose, etc material blending, to improve the material surface adhesion and toughness, bonding strength and resistance to yellowing transparency has significant effect

Performance：

 High adhesion and toughness, abrasion resistance, good adhesion.

 Excellent low temperature toughness, excellent resistance to chemicals

 Colorless and transparent yellowing resistance 

 weather resistance and excellent leveling compatibility

Range of application and Suggestions

 Plastic vacuum plating primer, topcoat resin as the main resin content 15-40%

 UV adhesive resin, used for metal, glass, plastic and other products, content 10-50%

 Electronics, cosmetics, furniture cabinets board UV varnish injector, content 10-30%

 Screen printing inks, good adhesion and gloss, content 10-30%

 Other polymer adhesion and toughness modifier content 5-20%

Typical physical and chemical performance indicators

	Index Name
	Testing standards
	skills requirement

	Exterior
	YW356
	Colored clear transparent liquid

	Chroma（APHA）≤
	YW8
	maximum50

	Viscosity（60℃）CPS
	YW121
	8000～12000

	NCO（%）≤
	YW110
	0.1

	The content of polymerization inhibitor；ppm；≤
	YW15
	10

	 Index of refraction
	YW24
	1.477

	Pencil Hardness
	T6739
	3B

	Adhesion（One hundred cells Crosshatch）
	T5210
	0（100/100）

	Resistant to boiling water（100℃，90minute）
	YW101
	No blistering and shedding


No blistering and shedding

A cool dry environment, 12 months

地址：广州市天河区中山大道旭景西街202号1402#    电话：020 – 29079054  传真：020 – 61208470  1973709656@qq.com； www.gztongy.cn


