广州同怡新材料科技有限公司


YWU2901
 Product introduction

  YWU2901 is di-functional polyurethane acrylic oligomer, the molecular weight between 2500-3500, molecular weight, high cohesive energy, stick relay is strong, show the material macro excellent performance, such as excellent adhesion and plated, high gloss and yellowing resistance and chemical resistance, because the main functional groups containing allyl base double bond, can radiation curing or chemical crosslinking, products with shallow transparent color, high adhesion, resistance to scratch, no yellowing highlights; Application scope wide, can separate as main resin used for UV light curing coatings, inks and adhesives and other products, and can and other acrylic system, epoxy, polyurethane, nitrocellulose, etc material blending, to improve the materials on the adhesion and plating, bonding strength and resistance to yellowing transparency has significant effect.
Performance：

High adhesion and plating, good adhesion, good wear resistance.

Good water resistance, good resistance to chemicals

Colorless transparent resistance to yellowing, good weatherability

Good flow property and intermiscibility

ange of application and Suggestions

Resin coated in plastic vacuum plating primer, as main resin, content of 15-40%

Can adhesive, and other acrylic acid, epoxy, polyurethane blend, used for metal, glass, plastic products, such as dosage of 10-20%

Electronics, cosmetics, furniture cabinet plate UV spray finishing, dosage of 10-30%

Screen printing ink, good adhesion and gloss, dosage of 10-20%

Other polymer flexibility and gloss modified agent, the dosage of 5-20%

Typical physical and chemical performance indicators

	Index Name
	Testing standards
	skills requirement

	Exterior
	YW356
	Colorless transparent liquid

	Chroma（APHA）≤
	YW8
	maximum50

	Viscosity（60℃）CPS
	YW121
	20000～30000

	 Index of refraction
	YW24
	1.4465

	Tg  (℃)
	DMA
	55℃

	Pencil Hardness
	T6739
	2B

	Adhesion（One hundred cells Crosshatch）
	T5210
	0（100/100）

	Resistant to boiling water（100℃，90minute）
	YW101
	No blistering and shedding


No blistering and shedding

A cool dry environment, 12 months

地址：广州市天河区中山大道旭景西街202号1402#    电话：020 – 29079054  传真：020 – 61208470  1973709656@qq.com； www.gztongy.cn


